## Slide 1: Copper and Bronze
https://www.youtube.com/watch?v=-JunmomMSK0

## Slide 2: Copper and bronze
What are properties of copper and bronze?
  Metallic
  Malleable
  Opaque
  Electrically conductive
  Thermally conductive
  Orange
  Shiny
  Hard

## Slide 3: Copper vs Bronze
Copper
  Is a pure element
  Named after where it came from Cyprus (Cu)
  Melting point around 1084*C
Bronze
  Is an alloy of copper and an impurity (Arsenic or Tin)
  Named after the Italian word Bronzo for bell Metal
  Melting point varies but around 950°C

## Slide 4: The Bronze Age
The early story of copper likely involved the role of serendipity—finding raw copper samples or inadvertently placing copper containing ores near or in a fire.
In the course of generating higher temperatures, early metal workers empirically developed the process of smelting.
Smelting provides increased temperatures as well as the pathway to a specific chemical reaction instrumental in removing (reducing) metals from their ores.
http://www.supplierlist.com/prod_img/qiguoying/21961_Elegant_Ancient_Bronze_Cooking_Vessel_From_China.jpg
This course contains copyright materials that are used solely for instructional purposes within this course. Copying, printing or distribution for other purposes is prohibited
Notes: What did you think of the books?
What is your opinion of the respective writing styles? Organizations?
What did you learn from reading two accounts of the same period? Did you notice differences in emphasis?

## Slide 5: Smelting
Until now the ancient materials we have discussed did not change oxidation state
To make a metal other than Gold typically requires reducing it chemically
For copper the reaction is simple
Take malachite (CuCO3) and carbon (charcoal) heat and copper will form
140 pounds of wood makes 20 pounds of charcoal along with which in turn makes 1 pound of Copper
  Resource intensive
  Must find lots of copper ore

## Slide 6: Smelting
Common smelting practices call for the mixing of ore with charcoal.
The incomplete combustion of the charcoal produces carbon monoxide.
Carbon monoxide reacts with the ore to produce carbon dioxide and elemental metal.
Be prepared to write the chemical equations describing the smelting of a copper oxide ore.
Notes: What did you think of the books?
What is your opinion of the respective writing styles? Organizations?
What did you learn from reading two accounts of the same period? Did you notice differences in emphasis?

## Slide 7: Why call it the Bronze age?
Copper
  Hardness of ~80 Mpa
  Yield Strength 70MPa
Bronze
  Hardness of 170MPa
  Yield Strength ~220MPa
  Why is Bronze harder and stronger?

## Slide 8: Strengthening Mechanisms
Copper was relatively easy to refine
However it is also very soft
There are multiple methods of strengthening
The key is slowing down dislocation motion
What’s a dislocation?
http://depts.washington.edu/matseed/mse_resources/Webpage/Metals/metalproperty.htm
Dislocation

## Slide 9: How do you slow down a dislocation?
Work Hardening
  Add lots of additional dislocations
  They get tangled
  Makes it difficult for them to move
  Cold rolling copper increases the tensile strength
http://www.australwright.com.au/c11000-etp-copper/
http://www.eng.nus.edu.sg/EResnews/022011/rd7.html

## Slide 10: How else do you strengthen Copper
Impurities
  Lots of hardening mechanisms
  Solid solution hardening is one
  Put other atoms into the matrix that block the dislocations
  Early on used Arsenic
  Later used Tin
https://en.wikipedia.org/wiki/Strengthening_mechanisms_of_materials
Maximum Yield Strength (MPa)
Impurity
http://www.tf.uni-kiel.de/matwis/amat/iss/kap_8/backbone/r8_3_1.html

## Slide 11: What happens when you add an Impurity? Need a Phase Diagrams
Water sugar phase diagram
Critical for making Ice Tea!

## Slide 12
Cu-As Bronze Phase Diagrams
Binary (2-component) phase diagrams (e.g. Cu-As) typically consider composition (x) versus temperature (y) behavior
In this phase diagram, only solids and liquids appear.
Solid lines still represent the separation between distinct phases.
Ancient Bronze
http://www.himikatus.ru/art/phase-diagr1/As-Cu.php
Melting point
Notes: What did you think of the books?
What is your opinion of the respective writing styles? Organizations?
What did you learn from reading two accounts of the same period? Did you notice differences in emphasis?

## Slide 13
http://pwatlas.mt.umist.ac.uk
Cu-Sn Bronze Phase Diagrams
Copper-Tin Bronze
Can dissolve more Tin in Cu than As
Tin is less toxic
Tin is harder to find
solubility
Notes: What did you think of the books?
What is your opinion of the respective writing styles? Organizations?
What did you learn from reading two accounts of the same period? Did you notice differences in emphasis?

## Slide 14
With the desire for improved properties, early coppersmiths likely began to draw correlations between copper sources, processing conditions, and resulting mechanical properties.
Different regions of the world are know to contain copper deposits of varying purity as well as being composed of various impurities.
The Bronze Age
Where is Copper?
Common impurities include arsenic and tin, separately found in different samples.
Notes: What did you think of the books?
What is your opinion of the respective writing styles? Organizations?
What did you learn from reading two accounts of the same period? Did you notice differences in emphasis?

## Slide 15: The Bronze Age
Arsenic is naturally found in many copper deposits.
The presence of arsenic will produce an altered color as well as increasing the hardness of copper.
Arsenic possesses a lower melting point that copper and preferentially oxidizes during smelting, producing the toxic chemical AsO3.
Notes: What did you think of the books?
What is your opinion of the respective writing styles? Organizations?
What did you learn from reading two accounts of the same period? Did you notice differences in emphasis?

## Slide 16: The tensile strength of copper tin alloys
Shepherd and Upton, J. Phys. Chem, 9, 441, (1905)
Adding Tin increases the strength
Heat treating also changes strength.
Adding too much tin is bad Why?

## Slide 17: THE BRONZE AGE
As has been mentioned, our historical records are incomplete with regard to the development and implementation of early materials. Yet it is known that many materials saw parallel discoveries and developments in different parts of the world.
Near East 3300BC
Europe 3000BC
China 3000BC
India 3300 BC
England 2100BC
Korea 800BC
Japan 500BC
Peru 100AD www. Wikipedia.com
Notes: What did you think of the books?
What is your opinion of the respective writing styles? Organizations?
What did you learn from reading two accounts of the same period? Did you notice differences in emphasis?

## Slide 18: THE BRONZE AGE
What were the societal impacts associated with the development of the material bronze?
Health
Mining
Exploration and experimentation
Trade
Cornwall England was the primary early source of tin in central and northern Europe as far back as 2000BC
Notes: What did you think of the books?
What is your opinion of the respective writing styles? Organizations?
What did you learn from reading two accounts of the same period? Did you notice differences in emphasis?

## Slide 19: Bronze age Map
Wikipedia.com
https://s-media-cache-ak0.pinimg.com/736x/ba/71/7a/ba717a4069f76031457d1d0e5b198c0b.jpg

## Slide 20: Bronze age Map
Wikipedia.com
https://s-media-cache-ak0.pinimg.com/736x/ba/71/7a/ba717a4069f76031457d1d0e5b198c0b.jpg
https://en.wikipedia.org/wiki/Tin_sources_and_trade_in_ancient_times
Where the Bronze was made
Where the Tin was mined
Trade was critical to the success of Bronze

## Slide 21: Otzi
3300BC
Oldest Chalcolithic Mummy
Found in 1991 in the Alps northern Italy
Under ice for 5000 years
High levels of both copper particles and arsenic were found in Ötzi's hair. This, along with Ötzi's copper axe which is 99.7% pure copper, has led scientists to speculate that Ötzi was involved in copper smelting
wikipedia
Otzi’s Axe
http://a57.foxnews.com/img.foxnews.com/static/managed/img/Scitech/660/371/OetzitheIceman02.jpg
https://s-media-cache-ak0.pinimg.com/236x/c6/41/3a/c6413aaa207762a1bb5f546ebb2eb249.jpg

## Slide 22: Early Bronze
1000BC King Solomans Temple
Built by Hyram of Tyree
39 feet tall
Pillaged
http://endtimelect.com/2013/02/02/the-two-pillars-boaz-and-jachin-the-entrance-to-the-temple-of-yhwh/

## Slide 23: THE BRONZE AGE
The development of bronze enabled casting technologies for the production of vessels, art, tools, and weapons.
http://www.supplierlist.com/prod_img/qiguoying/21961_Elegant_Ancient_Bronze_Cooking_Vessel_From_China.jpg
http://history.cultural-china.com/chinaWH/images/exbig_images/fa72017a6d174c8307fde4ea4f178dbd.jpg
http://www.wushumuseum.com/upload_files/image/200906/200906090943577070.jpg
Notes: What did you think of the books?
What is your opinion of the respective writing styles? Organizations?
What did you learn from reading two accounts of the same period? Did you notice differences in emphasis?

## Slide 24: Molds for making Bronze Swords 900BC in Ireland

## Slide 25: Mold for making Bronze Axe 900-500BC Ireland

## Slide 26: Bronze Crocodile Go Gators
Ancient Egypt